## Slide 1: Evaluation of In-Service Field Performance of High Polymer-Modified Asphalt Concrete Overlays
2024 Nevada Transportation Conference, Session 3
Tuesday, May 7th, 2024
Jhony Habbouche, Ph.D., P.E.
Senior Research Scientist – Pavements
Virginia Transportation Research Council (VTRC)

## Slide 2: Introduction Virginia’s Network
Interstates: > 1,000 of 5,000 lane-miles of asphalt over jointed concrete pavement (JCP)
Primary network: > 1,100 of 22,000 lanes-miles of asphalt over JCP
3rd largest US public roadway network

## Slide 3
Introduction High Polymer Modified Asphalt (HP) Mixtures
HP mixtures may offer additional advantages in flexible pavements subjected to heavy & slow moving traffic loads.
  New Construction: Consideration to fatigue cracking, rutting & shoving in AC layer, total rutting, and top-down cracking
  Rehabilitation (AC Overlay): Consideration to Reflective Cracking

## Slide 4
Background State-of-the-Practice

## Slide 5
Currently uses and/or previously experienced HP
material + Survey Responses Received
Currently uses and/or previously experienced HP
material + Survey Responses Not Received
No previous experience with HP material +
Survey Responses Received
No available literature on previous experience with HP material + Survey Responses Not Received
State-of-the-Practice Survey of US Transportation Agencies

## Slide 6
The technical help provided by the polymer supplier was very beneficial; the contractors learned a lot about how to handle and store the HP binder.
It is recommended that the contractors have other options if tank storage time becomes an issue, such as using HP binders in other applications or blend down options.
It is recommended that HP AC mixtures be kept out of low production or handwork areas unless absolutely necessary.
A material transfer device must be used to help contractors better establish a continuous paving process to produce a higher quality and smoother mat.
State-of-the-Practice Lessons Learned and Best Practices

## Slide 7
The in-line pipe diameters at the mix plant should be checked prior to delivery of HP asphalt binders; if needed, larger pipe diameters must be used.
Wax-like products, typically used to reduce binder viscosity, are not recommended.
Communication between the mix plant personnel and the supplier of the binder is considered essential to ensure there is no delay in production given the tendency of the HP asphalt binder to thicken quickly.
The quality of HP binder after delivery to the contractor should always be checked with respect to required specifications.
State-of-the-Practice Lessons Learned and Best Practices

## Slide 8
State-of-the-Practice Construction Practices: Experience of VA Contractors

## Slide 9
Definition and acceptance of HP binders is not related to SBS polymer content.
Performance-oriented viewpoint: definition related to specific binder rheology-related parameters and characteristics.
Agency | Standard / Test Method | Properties / Comments
Nevada | AASHTO T 315 AASHTO T 350 Nev. T746F | PG 70-34NV Jnr, 3.2 ≤ 0.1 kPa-1 and R3.2 ≥ 90% at 70ºC Original ductility at 4ºC, 5cm/mm ≥ 20 cm PAV-aged G*sinδ ≤ 4,000 kPa
Virginia | AASHTO T 332 AASHTO T 350 | PG 76E-28 Jnr, 3.2 ≤ 0.1 kPa-1 and R3.2 ≥ 90% at 76ºC
Background Definition and Specifications

## Slide 10
Year | Comments: Mix Type / District | Quantity of HP AC Mixes Produced (tons) | 
 |  | Specific per Mix Type & District | Total
2014 | SM-9.5 / NOVA (trial section) | -- | --
2015 | SM-9.0 / NOVA | 4,808 | 44,084
 | SM-12.5 / NOVA | 31,972 | 
 | SMA-9.5 / NOVA | 7,304 | 
2016 | SM-12.5 / NOVA | 5,643 | 11,848
 | SMA-9.5 / Richmond | 6,205 | 
2017 | SM-12.5 / Hampton Roads | 11,726 | 69,744
 | SMA-12.5 / Hampton Roads | 24,005 | 
 | SM-9.5 / NOVA | 3,904 | 
 | SM-12.5 / NOVA | 25,954 | 
 | SM-12.5 / Richmond | 4,155 | 
2018 | SM-9.5 / NOVA | 974 | 12,635
 | SM-12.5 / NOVA | 11,661 | 
2019 | SM-9.0 / NOVA | 17,724 | 65,923
 | SM-9.5 / NOVA | 6,598 | 
 | SMA-9.5 / NOVA | 41,601 | 
Background HP AC Mixtures in Virginia: Types & Quantities

## Slide 11: Objective & Scope of Work
Assess the viability of using HP AC mixtures in Virginia as a reflective cracking mitigation technique or as a tool for increased crack resistance on higher volume facilities:
Providing information on the state of practice in Northern America
Evaluating the performance characteristics of PMA and HP plant produced mixtures placed in Virginia
Compiling and analyzing PMS data for relevant in-service HP and several PMA pavements in Virginia
Determining the life expectancy of HP AC overlays

## Slide 12
In-Service Field Performance HP and PMA Selected Routes
No. | Route | County / County Mileposts | Pavement Type | Activity |  | Year of Prior Rehabilitation
 |  |  |  | Details | Year | 
1 | I-95SB | Prince William, 0.02-3.89 | BOJ | SM-12.5 E(HP) 2.0 in | 2015 | 2009
2 | I-95SB | Prince William, 10.98-13.12 | BOJ | SMA-9.5 E(HP) 1.5 in SMA-9.0 E(HP) 1.0 in | 2015 | 2007
3 | I-95NB | Prince William, 0.07-3.92 | BOJ | SM-12.5 E(HP) 2.0 in | 2015 | 2008
4 | I-495NB | Fairfax, 5.56-6.63 | BOJ | SM-12.5 E(HP) 2.0 in | 2016 | 2012
5 | I-95SB | Hanover, 2.76-5.63 | BOJ | SMA-19.0 E 2.0 in SMA-12.5 E(HP) 1.5 in | 2016 | 2002
C6 | I-95NB | Henrico, 7.33-9.55 | BOJ | SMA-9.5 E 1.5 in SMA-19.0 E 2.0 in | 2015 | 2004
7 | I-64EB | York, 14.81-20.55 | BOJ | THMACO 0.75 in SMA-12.5 E(HP) 2.0 in | 2017 | New Construction
8 | I-64WB | York, 14.98-20.33 | BOJ | THMACO 0.75 in SMA-12.5 E(HP) 2.0 in | 2017 | New Construction
9 | I-95NB | Fairfax, 3.41-4.45 | BIT | SM-12.5 E(HP) 2.0 in | 2017 | 2010
10 | I-495NB | Fairfax, 1.194-3.66 | BOJ | SM-9.0 E(HP) 1.0 in SMA-9.5 E(HP) 1.5 in | 2018 | 2014
11 | I-95NB | Prince William, 11.121-12.64 | BOJ | SM-12.5 E(HP) 2.0 in | 2018 | 2011

## Slide 13
In-Service Field Performance BOJ Section No.1

## Slide 14
In-Service Field Performance BOJ Section No.1, Cont’d

## Slide 15
In-Service Field Performance BOJ Section No.2

## Slide 16
In-Service Performance Life Analysis (i), BOJ Section No.1

## Slide 17
In-Service Performance Life Analysis (i), BOJ Section No.5 & C6, Approach I

## Slide 18
In-Service Performance Life Analysis (ii), Approach I
SM-PMA vs. SM-HP vs. SMA-PMA vs. SMA-HP

## Slide 19
In-Service Performance Life Analysis (ii), Approach II
SM-PMA vs. SM-HP vs. SMA-PMA vs. SMA-HP

## Slide 20
PMA vs. HP AC Mixtures
In-Service Performance Life Analysis (iii), Approach I

## Slide 21
PMA vs. HP AC Mixtures
In-Service Performance Life Analysis (iii), Approach II

## Slide 22: Summary of Findings & Conclusions
According to the PMS distress data, all of the evaluated mixtures (HP or PMA) had some degree of reflective cracking.
CCI values were higher and CCI loss rates were lower during the service life of HP overlays when compared with the PMA overlays.
Based on the collected and documented PMS data, HP sections showed very promising performance after 5 years (2015-2020) regardless of the traffic level and pre-existing pavement conditions.
The HP and PMA AC overlays had an average predicted service life of 8.3 and 6.2 years (Approach I), and 6.0 and 4.7 years (Approach II), respectively, indicating ~ 34% extension of performance life of the AC overlay with HP modification.

## Slide 23: Evaluation of In-Service Performance of Highly Polymer-Modified Asphalt Concrete Overlays
For more information:
Habbouche.jhony@gmail.com