## Slide 1: Ground Tire Rubber (GTR) in Asphalt Pavements: pros & cons, past, present, and a glimpse into the future
By Dr. Codrin Daranga
Paragon Technical Services Inc.
NTC Las Vegas, NV - May 2024

## Slide 2: Presentation Overview
Introduction
Background
How do we use GTR in asphalt
  Past
  Present
  Future?
Practical considerations
Summary

## Slide 3: Presentation Overview
Introduction
Background
How do we use GTR in asphalt
  Past
  Present
  Future?
Practical considerations
Summary

## Slide 4: Introduction
Recycling: Process of converting waste materials into now materials or objects.
Alternative to conventional waste disposal, saves material and reduces environmental impact.
Recycling of rubber from waste
tires into asphalt pavements
is an attractive alternative
addressing engineering, economic,
and environmental issues.
Triune Benefits of Recycling and Reuse
Notes: Recycling is the process of converting waste materials into new materials or objects. It is an alternative to conventional waste disposal that can save material and reduce environmental impact.
Recycling of rubber from waste tires is commonly referred to as recycled tire rubber or RTR. When used to modify asphalt binders and mixtures it is referred to as Ground Tire Rubber (GTR). Whether through binder or mixture modification, incorporation of GTR into asphalt pavements is an attractive alternative addressing engineering, economic and environmental issues.
The Federal Highway Administration (FHWA) established the FHWA Recycled Materials Policy regarding sustainable infrastructure in 2006. The FHWA policy states that recycling and reuse can offer triune benefits of “engineering, economic and environmental impact.”

## Slide 5: Introduction
The Federal Highway Administration (FHWA) Recycled Materials Policy:
Established in 2006.
Recycling and Reuse offers triune benefits of engineering, economic, and environmental impact.
Comparatively, (ASCE), sustainability is made up of environmental, social, and economic needs, collectively referred to as the “Triple Bottom Line.”
In-service asphalt pavement performance affects every facet of the FHWA recycled materials policy.
Federal Highway Administration (FHWA) project: “Deployment and Development of Innovative Asphalt Pavement Technologies. (DDIAPT)”
    Resource Responsible (RR) use of Materials for Flexible Pavement
    Technical Report – Resource Responsible Use of Recycled Tire Rubber in Asphalt Pavements https://scholarworks.unr.edu/handle/11714/7484
Notes: As stated, the Recycled Materials Policy regarding sustainable infrastructure was established by the Federal Highway Administration (FHWA) in 2006.
The policy states that recycling and reuse can offer triune benefits of engineering, economic and environmental impact. Comparatively the American Society of Civil (ASCE) state that sustainability is made up of environmental social, and economic needs referred to at the “Triple Bottom Line.”
Pavements with longer service lives should involve less maintenance and are environmentally friendly from the perspective that they involve less greenhouse gas; generating less attention per unit of use.
Pavements with longer service lives are more economical, and more efficiently serve public needs, which increases social well-being.
The primary objective of this report is to provide knowledge for resource responsible use of recycled tire rubber (RTR) in production of asphalt pavements and to promote sustainable use of recycled tire rubber in asphalt pavements. Technical information is given on the background of recycled tire rubber use in asphalt pavements and information related to specifications and testing of GTR-modified asphalt binders as well as considerations for GTR-modified asphalt mixture designs.
This project is sponsored by the Federal Highway Administration (FHWA) project: “Deployment and Development of Innovative Asphalt Pavement Technologies. (DDIAPT)” specifically related to “Resource Responsible (RR) use of Materials in Flexible Pavement” An accompanying Technical Report entitled “Resource Responsible Use of Recycled Tire Rubber in Asphalt Pavements” is also available: https://scholarworks.unr.edu/handle/11714/7484

## Slide 6: Presentation Overview
Introduction
Background
How do we use GTR in asphalt
  Past
  Present
  Future?
Practical considerations
Summary

## Slide 7: Typical Tire Components
Production of pneumatic tires for passenger cars, trucks, airplanes, etc. uses large quantities of polymers:
    Natural Rubber (NR),
    Synthetic Styrene Butadiene Rubber (SBR),
    Ethylene Propylene Diene Monomer (EPDM) Rubber,
    Butyl Rubber (BR)
Component | Typical Range
Natural rubber (NR) | 14 to 27 percent
Synthetic rubber | 14 to 27 percent
Carbon black | 28 percent
Steel, fabric | 14 to 15 percent
Processing oils and additives | 16 to 17 percent
Source PTSi
Notes: Typical Tire Components.
Large amounts of polymers, such as natural rubber (NR), synthetic polymers such as styrene butadiene rubber (SBR), ethylene propylene diene monomer (EPDM) rubber, and butyl rubber (BR), collectively referred to as rubber, are used in production of pneumatic tires for passenger cars, trucks, and aircraft, among others.

## Slide 8: Waste Tire Issue
At the end of serviceable life, discarded waste tires contain as much as 99% of the total rubber used in tire construction.
Environmental concern as polymeric materials do not decompose easily.
Two major challenges:
  Waste of valuable rubber,
  Environmental pollution due to disposal of waste tires.
Notes: Almost the entire amount of original rubber from a waste tires is discarded, which necessitates a very long time for natural degradation.
Disposal of waste polymers is a serious environmental concern as polymeric materials do not decompose easily.
This poses two major challenges: waste of valuable rubber and environmental pollution due to disposal of waste tires.

## Slide 9: Waste Tire Issue
Market or Disposition | Thousands of Tons | Millions of Tires | % of Total to Market
Tire-Derived Fuel (TDF) | 1,736.3 | 105.9 | 50.9
Cement Kilns | 805.9 | 49.2 | 23.6
Pulp & Paper | 503.1 | 30.7 | 14.8
Industrial Boilers | 427.3 | 26.1 | 12.5
Ground Tire Rubber (GTR) | 1,013.3 | 61.8 | 29.7
Civil Engineering (CE) | 316.0 | 19.3 | 9.3
Exported | 109.8 | 6.7 | 9.3
Electric Arc Furnace | 39.2 | 2.4 | 3.2
Reclamation Projects | 44.0 | 2.7 | 1.2
Agricultural | 7.1 | 0.4 | 1.3
Baled Tires/market | 14.6 | 0.9 | 0.2
Punched/ Stamped | 22.5 | 1.4 | 0.4
Other | 108.5 | 6.6 | 0.7
Total to Market | 3,411.3 | 208.1 | 100.0
Generated | 4,189.2 | 255.6 | –
% to Market/Utilized | 81.4% | 81.4% | –
Landfill Disposal | 646.8 | 39.5 | –
% Managed (Includes Markets, Baled, and Landfill) | 96.9% | 96.9% | –
Source USTMA
Notes: In 2017, as reported in the accompanying technical report, the US Tire Manufacturer’s Association (USTMA) reported that markets for scrap tires were consuming just over 3.4 million tons, or 81.4 percent, of the estimated 4.2 million tons of scrap tires generated annually.

## Slide 10: Waste Tire Issue
In 2017 Scrap Tire Markets consumed 81.4 percent of the estimated 4.3 million tons of scrap tires generated annually.
Chart: 
| Tire-Derived Fuel | Ground Tire Rubber | Civil Engineering
 | 0.509 | 0.297 | 0.093
Waste Tire Issue
Notes: The three largest scrap tire markets in 2017 were:
Tire-derived fuel (TDF), 50.9 percent, consisting of cement kiln, pulp and paper, and industrial boiler applications.
GTR, 29.7 percent, in asphalt, automotive, molded/extruded products, playgrounds/mulch, and sports surfacing applications.
Civil engineering (CE), 9.3 percent, including tire shreds used in road and landfill construction, septic tank leach fields and other construction applications.

## Slide 11: Waste Tire Issue
The GTR market is reported at slightly more than 1.0 million tons or about 62 million scrap tires.
Chart: 
| Asphalt | Automotive | Molded/Extruded Products | Playgrounds/Mulch | Sports Surfacing
 | 119 | 32 | 386 | 243 | 234
Notes: Recycling of waste rubber from tires into GTR involves grinding or reduction of tire rubber into smaller particle size, which results in an increase in surface area.
The rubber grinding industry classifies GTR according to particle size as rubber which is 2.0 mm (10 mesh) and smaller. The typical sizes of GTR used in modified asphalt binders and mixtures for pavement construction range from about 1.5 mm (1500 μm) down to 0.42 mm (420 μm) (14 mesh to 40 mesh), with limited use sizes as small as 177 μm (80 mesh) and 125 μm (120 mesh).
The GTR market is reported at slightly more than 1.0 million tons or about 62 million scrap tires. GTR-modified asphalt pavements represent 11.7 percent, or approximately 119 thousand tons (7.2 million scrap tires)

## Slide 12: Presentation Overview
Introduction
Background
How do we use GTR in asphalt
  Past
  Present
  Future?
Practical considerations
Summary

## Slide 13: Historical Perspective
More than 50 years of success in GTR modification of asphalt binders.
GTR modification of asphalt binders ranks second among polymer modifiers.
Modern GTR asphalt modification began in the early 1960s,
  Asphalt Rubber (AR) modified chip seal Phoenix, AZ,
  AR expanded into greater chip seal usage, crack relief interlayers and open-graded friction courses (OGFC)
  During 1960s through 1970s AR proved useful in asphalt pavements and pavement maintenance.
Notes: Research on GTR-modified asphalt binders over the last 50 years has shown favorable impacts of GTR modification. GTR ranks second among the most common asphalt polymer modifiers, behind styrene-butadiene-styrene (SBS) block copolymers.
Modern GTR use in paving began in the early 1960s with a highly elastic Asphalt Rubber (AR)
The work expanded into larger chip seal projects along with other crack relief interlayers, and open-graded surface courses.
During the two decades following, AR materials increased as they proved useful in various pavement maintenance functional applications including asphalt pavement, but by far the greatest utilization during this time frame was maintenance applications

## Slide 14: Historical Perspective
During 1960s through 1970s dry mixture addition of GTR emerged.
More issue with early dry mixture addition than dry addition today
  Rubber Modified Asphalt Concrete (RUMAC) – 10 mesh at 3 percent by weight of mix.
  PlusRideTM
  TAKTM
Dry addition of GTR to mixtures today consists of smaller sized rubber and lower rubber content – 30 mesh at 0.5 percent by weight of mix (10 percent of binder based on 5.0 percent binder content)
Dry addition technology today generally employs co-additives
Notes: During this same timeframe, versions of dry mixture addition of GTR to asphalt mixtures posed more of an issue than dry processes employed today.
These systems were collectively referred to as Rubber Modified Asphalt Concrete (RUMAC) (Buncher 1995).
The primary difference between the dry-process technologies of the 1960’s and 1970s compared to today’s dry-process technologies relates to GTR particle size and GTR dosage. Additionally, co-additives that aid in mixing, placement, and compaction have been employed. These additives have included processing aids from the tire manufacturing industry, Fischer-Tropsch waxes, and stearamide waxes.

## Slide 15: Presentation Overview
Introduction
Background
How do we use GTR in asphalt
  Past
  Present
  Future?
Practical considerations
Summary

## Slide 16: Current Usage
State DOT published specifications revealed that only twelve States currently publish specifications allowing GTR-modified asphalt binders for use in construction of asphalt pavements.
Notes: As of July 2021, a review of State DOT published specifications revealed that only twelve States currently publish specifications allowing GTR-modified asphalt binders for use in construction of asphalt pavements.

## Slide 17: Current Usage
State | Tons of GTR Used | % of Total Tons of GTR Used
Arizona | 4,303 | 21.4
Arkansas | 5 | <0.1
California | 13,412 | 66.7
Delaware | 10 | <0.1
Florida | 136 | 0.7
Georgia | 378 | 1.9
Illinois | 750 | 3.7
Massachusetts | 710 | 3.5
Michigan | 55 | 0.3
Missouri | 260 | 1.3
Texas | 98 | 0.5
Total | 20,117 | 100.0
Notes: The National Asphalt Pavement Association (NAPA) recently reported that twenty-one producers from eleven States indicated using GTR in some asphalt mixtures.
The 20 thousand tons of GTR used reported by NAPA is about 17 percent of the 119,000 lbs of GTR reported by the USTMA to be used in modified asphalt binders.
The NAPA report did not include use of GTR in surface treatments, such as chip seals, which is a major source of consumption. NAPA reported that approximately 59 percent of the total asphalt mixture tonnage using GTR was in California, which mandates widespread use of GTR in asphalt pavements (not a Federal requirement)
California is by far the largest user of GTR-modified asphalt binder, with usage being directed by PRC 42703. The California DOT (Caltrans) requires (not a Federal requirement) that: GTR be derived from automobile and truck tires only; GTR-modified binders be homogeneous; GTR-modified binders may not contain visible rubber particles; and GTR-modified binders contain a minimum of 10 percent GTR.
Arizona, the second largest user of GTR-modified asphalt binders, has two different specifications, Crumb Rubber Asphalt (CRA) consisting of GTR modified binder with 20 percent minimum GTR content produced using the AR technology, and PG graded (AASHTO M320) for hybrid GTR produced by the rubber modified binder (RMB) technology with a minimum of 8 percent GTR and 2 percent SBS. Arizona’s hybrid GTR-modified binder specifications are designated as PG 64-28 TR+, PG 70-22 TR+ and PG 76-22 TR+

## Slide 18: Processes and Technologies
Currently there are two primary processes of incorporating GTR into asphalt binders and mixtures referred to as either the “wet” or “dry” process.
The wet process blends GTR with asphalt with one of two technologies:
Wet Process
Terminal Blend
The dry process incorporates GTR directly into the asphalt mixture during production
Notes: To understand the processing technologies discussed, this figure presents a chronology of GTR uses in asphalt binders and mixtures in the U.S. Currently there are two primary processes of incorporating GTR into asphalt binders and mixtures referred to as either the “wet” or “dry” process.
The wet process blends GTR with asphalt with one of two technologies. It is done either on-site at the asphalt mixture plant (Asphalt Rubber (AR)) or at the asphalt binder supply terminal (Rubber Modified Binder (RMB)), with a prescribed minimum reaction time or minimum acceptance specificaitons prior to mixing the GTR-modified asphalt binder with aggregate.
The dry process incorporates GTR directly into the asphalt mixture during production. This is usually done by adding the GTR directly to the aggregate in the asphalt plant mixing drum prior to introducing the asphalt binder.
These three technologies will be discussed in the following slides.

## Slide 19: Asphalt Rubber (AR)
Technologies Included in This Process | Technology Definition | Other Names of the Technology
Asphalt Rubber (AR) | “An asphalt binder in various types of flexible pavement construction including surface treatments and asphalt mixtures consisting of a blended asphalt binder, ground tire rubber (GTR), and certain additives in which the rubber component is at least 15 percent by weight of the total blend and has reacted in the asphalt binder sufficiently to cause swelling of the rubber particles.” | McDonald Process Arizona Crumb Rubber Wet Process Rubber Recycled Tire Rubber Modified Bitumen (RTR-MB) Asphalt Rubber Binder (ARB) Bitumen Rubber Binder Crumb Rubber Binder Batch Blending
Notes: Asphalt Rubber or AR is defined here as “An asphalt binder in various types of flexible pavement construction including surface treatments and asphalt mixtures consisting of a blended asphalt binder, ground tire rubber (GTR), and certain additives in which the rubber component is at least 15 percent by weight of the total blend and has reacted in the asphalt binder sufficiently to cause swelling of the rubber particles.”
Other names for this technology include, with appropriate acronyms: The McDonald Process, Arizona Crumb Rubber, Wet-Process Rubber, Recycled Tire Rubber Modified Bitumen (RTR-MB), Asphalt Rubber Binder (ARB) Bitumen Rubber Binder, Crumb Rubber Binder, and Batch Blending

## Slide 20: Rubber Modified Binder (RMB)
Technologies Included in This Process | Technology Definition | Other Names of the Technology
Rubber Modified Binder (RMB) | “A version of the wet process where ground tire rubber (GTR) is blended with asphalt binder at the refinery or at an asphalt binder storage and distribution terminal and transported to the asphalt mix plant or job site for use. These blends may contain from 5 to 12 percent GTR by total asphalt binder mass. Some hybrid RMB binders may contain polymers such as styrene-butadiene-styrene (SBS) in addition to GTR.” | Terminal Blend Terminal Blended Rubberized Asphalt (TBRA) Recycled Tire Rubber Modified Bitumen (RTR-MB) Rubber Modified Binder (RMB) Hybrid Rubber Binder Wright Process
Notes: Rubber Modified Binder or RMB is defined as, “A version of the wet process where ground tire rubber (GTR) is blended with asphalt binder at the refinery or at an asphalt binder storage and distribution terminal and transported to the asphalt mix plant or job site for use. These blends may contain from 5 to 12 percent GTR by total asphalt binder mass. Some hybrid RMB binders may contain polymers such as styrene-butadiene-s tyrene (SBS) in addition to GTR.”
Other names for this technology include, with appropriate acronyms: Terminal Blend, Terminal Blended Rubberized Asphalt (TBRA), Recycled Tire Rubber Modified Bitumen (RTR-MB), Rubber Modified Binder (RMB) Hybrid Rubber Binder, and the Wright Process.

## Slide 21: Dry Process Rubber
Technologies Included in This Process | Technology Definition | Other Names of the Technology
Dry Process | “A process where hot-mix asphalt mixture is modified with ground tire rubber (GTR) using GTR as an aggregate/binder modifier which is incorporated into the aggregate prior to mixing with asphalt binder producing a GTR-modified hot-mix asphalt mixture. GTR used in this technology is generally less than 0.6mm (30 mesh).” | Dry process rubber Belt add modifier (BAM)
Notes: Dry Processed Rubber is defined as: “A process where hot-mix asphalt mixture is modified with ground tire rubber (GTR) using GTR as an aggregate/binder modifier which is incorporated into the aggregate prior to mixing with asphalt binder producing a GTR-modified hot-mix asphalt mixture. GTR used in this technology is generally less than 0.6mm (30 mesh).”
Other names for this technology include, with appropriate acronyms: Dry-process Rubber, and Belt Add Modifier (BAM).

## Slide 22: Presentation Overview
Introduction
Background
How do we use GTR in asphalt
  Past
  Present
  Future?
Practical considerations
Summary

## Slide 23: Future: What does it look like?
Ideally, we will find a way to keep GTR from separating/settling in asphalt.
Maybe figure out how to get more participation from the polymers in GTR.
For RTR in general ideally would be to find a way back to the starting materials (no, de-vulcanization is not real, it is a stretching of the truth at best).

## Slide 24: Presentation Overview
Introduction
Background
How do we use GTR in asphalt
  Past
  Present
  Future?
Practical considerations
Summary

## Slide 25: Specifications and Testing of GTR-Modified Asphalt Binders – Wet Process
The Superpave asphalt binder specification (AASHTO M 320 Standard Specification for Performance-Graded Asphalt Binder) encourages wider use of rheology-based testing of GTR-modified asphalt binders using the wet process and either the AR or RMB technology.
The Multiple-Stress Creep and Recovery (MSCR) (AASHTO M 332 Standard Specification for Performance-Graded Asphalt Binder Using Multiple Stress Creep Recovery (MSCR) Test) testing may also be employed.
Notes: Specifications and Testing of Wet processed GTR-Modified Asphalt Binders
AASHTO Standard Specifications M 320 and M 332 may be employed for wet-processed GTR modified asphalt binders. Modifications to dynamic shear rheometer methods such as increased gap and concentric cylinder geometries have been used to address GTR particle size affects. Increased gaps and alternative geometries allow adherence to standard specifications.

## Slide 26: Specifications and Testing of GTR-Modified Asphalt Mixtures – Dry Process
Specification and certification of mixtures modified with GTR using the dry process is not as straightforward as when the wet process is used.
Some agencies have specified the GTR-modified asphalt binder be evaluated and certified via asphalt binder extraction, recovery, and subsequent testing of recovered asphalt binder when the dry process is used.
Notes: Specifications and Testing of Dry-Process GTR-modified Asphalt Mixtures.
Specification and certification of dry-process GTR modified mixtures is not as straight forward as with the wet-processes. While some agencies have specified binder be extracted from mixture for subsequent binder testing there are concerns with this practice.

## Slide 27: Specifications and Testing of GTR-Modified Asphalt Mixtures – Dry Process
Extracted asphalt binder testing poses one of two, possibly both, concerns:
  Is GTR/GTR modified asphalt binder totally recovered from the mixture,
  does solvent interaction incorporate rubber and asphalt binder in a manner not achieved in the in-place mixture.
Specification of the mixture using the dry process is possibly more appropriately based on mixture testing schemes such as the balanced mixture design (BMD) approach.
Notes: Two concerns are posed with testing of extracted binder from mixture:
1. Is the GTR totally recovered from the mixture along with the asphalt binder? GTR is not totally soluble in any solvent due to SBR content.
2. Does solvent extraction aid in better incorporation of the rubber and asphalt compared to actual field performance.
Balanced mixture design (BMD) mixture testing schemes may be more appropriate for evaluation of dry-process rubber modified mixtures.

## Slide 28: Practical considerations
Make sure the GTR particles “have room” in the mix design/aggregate gradation.
GTR even when in the binder it is NOT binder therefore it does not replace binder. For example: if using 10% by wt. GTR modified asphalt you really get more surface area to coat (aggregate plus GTR) with less binder (90% instead of 100%). Need to bump the AC content, usually by 0.2 to 0.5% AC in the mix.
Ensure proper equipment is available to prevent settlement and maintain binder homogeneity.

## Slide 29: Presentation Overview
Introduction
Background
How do we use GTR in asphalt
  Past
  Present
  Future?
Practical considerations
Summary

## Slide 30: Summary
Lacking the ability to recycle old tires into new tires, there are several common repurposing methods to effectively reuse rubber.
GTR is the second highest consumer of RTR with uses in:
  Molded and extruded products,
  Playground and mulch applications,
  Sports surfacing,
  Asphalt binder modification,
  Automotive uses.
Modification of asphalt binders with GTR is well established and can provide high performance pavements that aid in reduction of the number of waste tires disposed of in landfills and elsewhere.
Growth in use of GTR-modified asphalt pavements can be credited to successful construction of high-performance asphalt pavements

## Slide 31: Summary
GTR is being successfully used in Pavements in both wet and dry form.
Proper design needed to insure adequate performance
If specification do not allow it, it is not happening!
History of both good and bad performance can be found out in the real world going back for many years. NCAT, MnRoad and many more examples available in the real world of successful GTR containing pavements.